Fuel Cell

Author: Mariam El Rez

Editor: Samir Mourad

Last update: 30 December 2021

CONTENTS

List of figures	5

1.	Type of fuel cell	9

1.1.	Acid electrolyte fuel cell	9

1.2.	Alkaline electrolyte fuel cell	10

1.3.	Proton exchange membrane fuel cell	11

2.	Technical and physical description of a fuel cell	12

3.	Fuel cell stack	13

3.1.	Simple series connection	13

3.2.	Bipolar series connection	14

4.	Fuel cell system	18

5.	Energy efficiency, Power and Lifetime	19

6.	Manufacturing and environment	19

7.	Advantages and Drawbacks	20

8.	Components of PEMFC	20

9.	How Fuel Cells Work 	25

9.1.	Parts of a fuel cell	29

9.1.1.	Membrane Electrode Assembly	29

9.1.2.	Hardware	30

9.2.	Fuel cell systems	31

9.2.1.	Fuel Cell Stack	31

9.2.2.	Fuel Processor	31

9.2.3.	Power Conditioners	31

9.2.4.	Air Compressors	32

9.2.5.	Humidifiers	32

10.	Cell structure	32

11.	Analysis of quantities	34

11.1.	Fluidic quantities	34

11.2.	Thermal quantities	36

11.3.	Electric dynamic	37

12.	Parametric influence	38

12.1.	In the canals	38

12.2.	In the catalytic layer	39

12.3.	In the membrane	39

13.	Comparison of Fuel Cell technologies 	40

14.	Production process of PEM fuel cell components	41

15.	Overview of PEM fuel cell components	42

16.	Thermal Engineering Performance Evaluation of a Polymer Electrolyte Membrane Fuel Cell Stack at Partial Load 	43

16.1.	Thermal Engineering Analysis	44

16.2.	Experimental Method	46

16.3.	Cooling Performance	50

16.4.	Conclusions	51

17.	Consideration for Fuel Cell Design	52

17.1.	Fuel Cell Stack Size	52

17.2.	Number of Cells	53

17.3.	Stack Configuration	54

18.	Polymer Electrolyte Membrane Fuel Cells (PEMFCs)	56

18.1.	Basic stationary fuel cell calculations.	57

18.2.	Fuel Cell Reversible and Net Output Voltage	59

19.	Model creation of PEM fuel cell 	61

19.1.	Material and assembly (exp) 	62

19.2.	Experimental set-up and procedure 14	64

20.	Study of PEM Fuel Cell End Plate Design by Structural Analysis Based on Contact Pressure 	65

20.1.	Introduction	65

20.2.	Description of Geometry	66

20.3.	Boundary condition	68

21.	Components in a single cell	69

22.	Fuel cell stack	70

22.1.	Add cell to the stack	70

22.2.	Working prototype	79

23.	Fuel Cell Materials	82

23.1.	Electrolyte Layer	82

23.2.	Fuel Cell Electrode Layers - PEMFC catalysts	83

23.3.	PEMFC gas diffusion layers	83

24.	Constructing the Fuel Cell Bipolar Plates, Gaskets, End Plates, and Current Collectors	84

24.1.	Bipolar plate design	84

24.2.	Gasket selection	86

24.3.	End plates	86

25.	Conclusion of Fuel Cell components	87

26.	Bipolar plate design	88

27.	Components costs of one cell	91

27.1.	PEMFC	91

27.2.	MEA	92

21.2.1. Nafion for Electrolyte	96

21.2.2. Carbon paper for GDL	99

21.2.3. GDL+Catalyst	101

27.3.	Bipolar plate	101

27.4.	Gaskets	108

27.5.	Current plate	110

27.6.	End plate	110

28.	Description of our prototype fuel cell system	112

28.1.	Existing electrical system	112

28.2.	Fuel cell stack	112

28.2.1.	Size	112

28.2.2.	Fuel cell types	113

28.3.	Converters	113

28.3.1.	DC/DC converter	113

28.3.2.	DC/AC inverter	113

28.4.	Hydrogen storage	114

28.5.	Energy and fuel estimation	114

28.6.	FreeCAD design	114

28.6.1.	Bipolar plate design	114

28.6.2.	Gasket design	118

28.6.3.	MEA design	120

28.7.	Specification of requirements	121

References	124

# List of figures

Fig. 1 :Schematics of a fuel cell stack operation and components	8

Fig. 2 :Basic structure of a fuel cell.	9

Fig. 3:Electrode reactions and electrical flow for an acid electrolyte fuel cell. The electrons flow from the anode to the cathode via an external circuit.	10

Fig. 4:Electrode reactions and electrical flow for an alkaline electrolyte fuel cell.	11

Fig. 5: PEMFC	12

Fig. 6: Activation energy diagram for a simple exothermic chemical reaction.	13

Fig. 7:Simple series connection from the anode of one cell to the cathode of the next one.	14

Fig. 8: A fuel cell stack, consisting of three cells connected with bipolar plates.	15

Fig. 9:Structure of a fuel cell with edge seals to prevent leakage of the gas at the edges of the electrodes.	16

Fig. 10:Fuel cell stack with external manifolding	17

Fig. 11: Fuel cell stack with internal manifolding. A more complex bipolar plate is used to allow the reactant gases to be fed to the electrodes through internal channels.	18

Fig. 12: Current collector	20

Fig. 13: Gas diffusion layer for anode	21

Fig. 14 : Membrane electrode assembly	21

Fig. 15: Cathode gas diffusion layer	22

Fig. 16: Perforated metal plate	22

Fig. 17: Bipolar plate	23

Fig. 18: Single cell	23

Fig. 19: Stack of PEMFC	24

Fig. 20: Air inlet and cooling	25

Fig. 21: An exploded view of a fuel cell stack 	25

Fig. 22: Basic micro fuel cell based upon traditional fuel cell design 5	26

Fig. 23: Generalized schematic of a single fuel cell 	26

Fig. 24: Schematic of a PEM fuel cell stack 5	27

Fig. 25:A cross section of the PEM fuel cell. The unit cell is made of 7 layers which are made of different compositions of material providing the layers with different properties 	28

Fig. 26: PEMFC – flowing path of fuel and air	29

Fig. 27: Cell structure	32

Fig. 28: Structural setup	34

Fig. 29: Fluidic quantities (Pressure distributions & dynamics) variations in the canals	35

Fig. 30: Fluidic quantities (Distributions & dynamics) variations in the GDL	35

Fig. 31:Fluidic quantities (Distributions & dynamics) variations in the membrane	36

Fig. 32: Thermal quantities (Distributions & dynamics) variations in the electrode	36

Fig. 33: Electric dynamic (Distributions & dynamics) variations in the channel & the diffusion layer	37

Fig. 34: Electric dynamic (Distributions & dynamics) variations in the membrane	38

Fig. 35: Parametric influence in the canal	39

Fig. 36: Parametric influence in the catalytic layer	39

Fig. 37: Parametric influence in the membrane	40

Fig. 38: Comparison of Fuel Cell technologies	40

Fig. 39: Comparison of Fuel Cell type	41

Fig. 40: Production process of PEM fuel cell components	42

Fig. 41: Overview of catalyst coated membrane	42

Fig. 42: Overview of Gas diffusion layer (GDL)	43

Fig. 43: Overview of bipolar plate	43

Fig. 44: PEM fuel cell system specifications	46

Fig. 45:  Operating conditions of fuel cell	47

Fig. 46: The fuel cell system schematic	48

Fig. 47: Relation of stack temperature to electrical power	48

Fig. 48:The total stack thermal energy compared to combined cooling effects	49

Fig. 49: Relation of stack heat and stack-to-cooling water temperature profile	49

Fig. 50: Active and passive cooling contribution percentages	50

Fig. 51: Theoretical optimum cooling contributions of passive and active cooling	50

Fig. 52: Temperature profile at heat exchanger	51

Fig. 53: Effectiveness of the heat exchanger at steady-state	51

Fig. 54: Typical polarization curve for a PEM fuel cell stack.	53

Fig. 55: Typical fuel cell stack configuration (a two-cell stack)	55

Fig. 56: Physical characters of proton exchange membrane fuel cell (PEMFC)	56

Fig. 57: The polymer electrolyte fuel cell (PEMFC) 4	57

Fig. 58: Fuel cell heat and mass balance	60

Fig. 59: Simple PEM fuel cell system [5]	60

Fig. 60: Dimensions of PEM fuel cell model	61

Fig. 61: Model of serpentine channel flow field of PEM fuel cell	61

Fig. 62: The analysis was done with three different pressure (1 bar, 1.5 bar, 2 bar) and voltage (0.25 V-0.85 V) at constant temperature of 323 K (50oc) using Ansys and checked	62

Fig. 63: Assembly steps of the PEM fuel cell	63

Fig. 64: Material properties of the fuel cell component	63

Fig. 65: The Polymer Electrolyte Membrane Fuel Cell (PEMFC)	64

Fig. 66: Schematic of Polymer Electrolyte Membrane Fuel Cell showing different components 	65

Fig. 67: Condensation of water produced by a PEMFC on the air channel wall. The gold wire around the cell ensures the collection of electric current	65

Fig. 68: Schematic geometry of PEMFC	66

Fig. 69: Material properties of PEMFC components	67

Fig. 70: Components in a single cell	70

Fig. 71: Stack of the PEMFC from the anode & cathode side	70

Fig. 72: Remove the bolts and nuts from stack	71

Fig. 73: Remove the end plate from the stack	71

Fig. 74: Remove the current plate collector, with the gasket from the stack	72

Fig. 75: First cell next to the current collector	72

Fig. 76: Overview of a single cell (Two graphite plate and one MEA)	73

Fig. 77: The MEA layer	73

Fig. 78: Gas distribution channel with multiple support flow field, and field gasket at the front side	74

Fig. 79: Gas distribution channel with multiple support flow field, and field gasket at the back side	75

Fig. 80: Steps to build a cell	75

Fig. 81: Add the plate in the appropriate direction to the stack	76

Fig. 82: Add the gasket	76

Fig. 83: Add the MEA	77

Fig. 84: Add the second gasket	77

Fig. 85: Emplacing the plate through the tie rod	78

Fig. 86: Add the second cell	78

Fig. 87: Placed back the current collector	79

Fig. 88: Placed back the end plate	79

Fig. 89: Common Materials Used for Each Fuel Cell Type	82

Fig. 90: Cation Exchange Membrane Comparison Chart 	82

Fig. 91: Anode catalyst materials	83

Fig. 92: Carbon cloth and toray paper ( picture courtesy of Fuel Cell Scientific )	84

Fig. 93: Properties of Commercially Available Carbon Papers Used as Substrates In PEMFC Electrodes	84

Fig. 94: Properties of various types of bipolar plates for PEM fuel cells 	84

Fig. 95: Process Options for Bipolar Plates	85

Fig. 96: Bipolar plate design for hydrogen and air flow channels for a PEMFC	86

Fig. 97: Gaskets, end plate, and MEA for PEMFC	86

Fig. 98: End and flow field plates, gaskets, current collectors, and MEA for a single-cell PEMFC stack	87

Fig. 99: Resumed the materials needed for our fuel cell	88

Fig. 100: Sizing of our fuel cell design	90

Fig. 101: Voltage-current density diagram for a low temperature, air pressure fuel cell	112

Fig. 1 :Schematics of a fuel cell stack operation and components

An electric generator:

- The fuel cell transforms chemical energy into electrical energy;

- We have a fuel and an oxidizer as in a heat engine;

- Electric power is produced directly without an alternator.

The first fuel cell was demonstrated in the middle of the 19th century by a scientist named William Grove. In a fuel cell a reaction takes place where hydrogen and oxygen recombine into water and thereby releasing electrical energy. The chemical formula of the reaction is seen in equation 1.

(1)

A fuel cell consists of two electrodes, anode and cathode, with a layer of electrolyte between them, Figure 1. The electrodes are normally made flat and porous to achieve good contact between the electrolyte and the gases. The layer of electrolyte is made thin for the purpose to allow ions to pass through it without too much ohmic losses.

fig. 2 :Basic structure of a fuel cell.

- Type of fuel cell

There are many different fuel cell types. The differences between them are the reactions at the electrodes and the electrolyte used. In the following subparagraghs some of the most common types of fuel cells are explained briefly.

  - Acid electrolyte fuel cell

The most common type of fuel cell is the acid electrolyte, seen in Fig 3. At the anode the following reaction takes place.

(2)

Hydrogen gas ionizes into hydrogen ions and electrons, equation (2). The electrons released from the reaction flow through an external load to the cathode, creating a current. The H+ ions pass through the electrolyte which is possible because an acid is a fluid with mobile H+ ions. At the cathode the H+ reacts with oxygen and the electrons forming water, equation (3)

(3)

The electrons are not allowed to pass through the electrolyte because then no current would flow in the external circuit.

Fig. 3:Electrode reactions and electrical flow for an acid electrolyte fuel cell. The electrons flow from the anode to the cathode via an external circuit.

  - Alkaline electrolyte fuel cell

In the Alkaline electrolyte the reaction is similar to the acid electrolyte but the reactions at each electrode are different. In this case the mobile ions are hydroxyl ions (OH-). The hydrogen fuel reacts with OH- at the anode producing water and releasing electrical energy, equation (4).

(4)

At the cathode side the electrons released from the anode reacts with oxygen and water creating new OH- ions, equation (5). Although water is consumed at the cathode, twice the amount is produced at the anode.

(5)

As for the acid electrolyte there must be an external load so that the electrons can flow from the anode to the cathode, Figure 4.

Fig. 4:Electrode reactions and electrical flow for an alkaline electrolyte fuel cell.

Worth mentioning is that for both the acid electrolyte and the alkaline electrolyte twice as many moles of hydrogen as of oxygen are needed in the reaction.

  - Proton exchange membrane fuel cell

The Proton Exchange Membrane (PEM) fuel cell is the most useful at present time. A solid polymer, in which protons (H+) are mobile, is used as electrolyte. The fact that the electrolyte is solid and immobile makes this cell very simple. The working temperature of these cells is quite low, around 30 -100°C, which gives a problem of slow reaction rates but at the same time the startup is fast. The problem of slow reaction rates is solved by the use of more effective electrodes and catalysts such as platinum. Another drawback is that the membrane is fragile and breaks easily. The field of application is essentially in vehicles, portable applications and low power CHP (Combined Heat and Power) systems.

- There are currently 6 types of fuel cell:

• AFC (Alkaline fuel Cell),

• PEMFC (Proton Exchange Membran Fuel Cell),

• DMFC (Direct Methanol Fuel Cell),

• PAFC (Phosphoric Acid Fuel Cell),

• MCFC (Molten carbonate Fuel Cell),

• SOFC (Solid Oxid Fuel Cell).

- PEMFC

- Uses H2 as fuel (sometimes CH3OH)

- A polymer membrane

- Works at a low temperature (≈ 60˚C)

- Starts quickly

Fig. 5: PEMFC

- Technical and physical description of a fuel cell

Electrical energy is produced when hydrogen reacts at the anode and oxygen at the cathode. To release it, an activation energy must be supplied in order to overcome the energy hill. The reaction has the form shown in Figure 6. If the probability of a molecule having enough energy is low a slow reaction takes place. This is not the case for fuel cell reactions at very high temperatures. To speed up the reaction the most common solutions are:

- Increasing the electrode area

- The use of catalysts

- Raising the temperature

The latter two are applicable to any chemical reaction. The first one is the most important when working with fuel cells. For a reaction like the one in equation (4), fuel gas, OH- ions and the necessary activation energy are needed. The hydrogen fuel and OH- ions comes in contact on the surface of the electrode, and at the same time the produced electrons must be removed. The time that this take is reversed proportional to the area of the electrode, i.e., the larger the electrode area is the less time it takes. The area is such an important issue that the performance of a fuel cell is expressed in ampere/cm2.

Fig. 6: Activation energy diagram for a simple exothermic chemical reaction.

- Fuel cell stack

  - Simple series connection

A single fuel cell is made very thin for purposes stated before. This however limits the voltage across it. A typical value for the voltage is about 0.7 V when drawing a useful current. A higher voltage can be achieved by connecting several cells in series which is known as a stack. The easiest way of doing this is to connect the edge of the anode to the cathode of the next cell, Figure 7. With this configuration the electrons have to travel across the surface of the electrode to the edge. Even if the electrodes are good conductors there will be a voltage drop. This drop will be substantial in comparison to the low cell voltage and therefore this method is not used unless the current is very small.

Fig. 7:Simple series connection from the anode of one cell to the cathode of the next one.

  - Bipolar series connection

A better solution for the construction of a stack is to make the connections with bipolar plates made from materials with good conductivity such as graphite or stainless steel. These plates make connections all over one cathode to the anode of the next cell, hence bipolar. The conditions that they must fulfill are that there has to be a good electric connection between the electrodes and that the different gases must be separated.

In the bipolar plates there are normally horizontal channels used to feed oxygen to the cathode and vertical channels to feed hydrogen to the anode, Figure 8. When assembling the stack with bipolar plates a solid block is formed where the current flows more or less straight through the cells instead of across the surface, resulting in better efficiency. The block also becomes more robust and strong due to that the electrodes are better supported. The design of the bipolar plate is somewhat complex where a balance between electrical contact and gas flow has to be considered. If the contact points are made as large as possible optimization of the electrical contact is achieved, but then the gas flow is decreased over the electrodes. Small contact points are also possible but then they should be frequent which makes the manufacturing difficult and expensive as well as a fragile plate. To obtain low resistivity and a small stack size the bipolar plate should be made thin. This results in narrow channels which makes it harder for the gas to flow around the cell.

Fig. 8: A fuel cell stack, consisting of three cells connected with bipolar plates.

In reality, when designing a stack with bipolar plates further considerations have to be done. The difficulties include supply and leakage of the gases. As mentioned before the electrodes are made porous to allow the gas to pass through it. A result of this is that the gas can leak out of the edges of the electrodes. The solution to this problem is to seal the edges. This is done by making the electrodes smaller than the electrolyte and then fitting a sealing gasket around them, Figure 9.

Fig. 9:Structure of a fuel cell with edge seals to prevent leakage of the gas at the edges of the electrodes.

When supplying fuel and oxygen to a fuel cell stack, where the edges of the electrodes are sealed, four manifolds, one at each side, are used. Because of the seals the hydrogen fed vertically only comes in contact with the anodes and the oxygen fed horizontally only comes in contact with the cathodes. The arrangement can be seen in Figure 10, where the manifolds are not assembled. This is called external manifolding and the main advantage is the simplicity of it. However, there are two important disadvantages. The first one is the problem regarding the cooling of the system. It is difficult to supply some kind of extra cooling and therefore the cells have to be cooled using the air passing through the cathodes. This leads to that the air has to be supplied at a higher rate than necessary. In some cases, this is enough to cool the cells but energy is wasted. The second disadvantage concerns the gasket around the edges of the electrode. At the points where there is a channel it is not pressed down evenly which can cause a leakage of the gases.

Fig. 10:Fuel cell stack with external manifolding

A better, yet more complex bipolar plate is made with internal manifolding where the channels are located inside the plate. The plates are also made larger than the electrodes with extra channels running through the stack, as seen in Figure 11. The fuel and the oxygen are fed into the channels via holes placed at each corner of the end plates. A fuel cell stack with internal manifolding has the appearance of a solid block and the gases are fed where the positive and negative connections are made. This arrangement can be cooled in different ways. The easiest way is to drive cooling air or water through the stack by channels at the edges.

Fig. 11: Fuel cell stack with internal manifolding. A more complex bipolar plate is used to allow the reactant gases to be fed to the electrodes through internal channels.

- Fuel cell system

In a fuel cell system the stack is the main component but it is only one part of the whole system. The other components are often called the balance of plant (BOP). Elements such as pumps or blowers are used to circulate the air and fuel in the stack. Compressors can be used, sometimes together with intercoolers, as for internal combustion engines. To drive the pumps, blowers and compressors, electric motors are needed.

The output of a fuel cell stack is a direct current (DC) which is almost never suitable for direct connection to any load. Therefore some kind of power conditioning is needed. What kind of device that is used depends on the need of the load. It can be a DC/DC converter or a DC/AC inverter.

Some kind of fuel storage will always be a part of the system. In the case when the fuel used is not hydrogen a fuel processing system is needed, e.g., to produce hydrogen from fossil fuels.

Different control valves, pressure regulators and in most cases a controller for coordination of the system are needed. Start-up and shutdown of the fuel cell system are complex problems for the controller.

In larger fuel cell systems, a cooling system is necessary. In the case of CHP systems, it is called a heat exchanger which takes care of the excess heat and uses it for another application. When using high temperature cells, the generated heat is sometimes used in fuel or air pre-heaters. In PEM fuel cells the reactant gases are often humidified.

- Energy efficiency, Power and Lifetime

The energy efficiency from a fuel cell stack can be as high as 80%. For the total system the efficiency is lower. How high the efficiency is depending on the amount and what kind of components that are used. For a fuel cell car engine including the whole system, the efficiency from chemical input to kinetic energy is about 30 – 40%. For comparison it should be known that in a conventional internal combustion engine the same efficiency is typically around 18 – 22%.

The power drawn by the load is an important aspect for the lifetime of a fuel cell. A smoother power consumption, i.e., an even power outtake without that many peaks, is preferable. This gives a more durable fuel cell. Car engines can be used as an example to illustrate this. A normal internal combustion engine could be assumed to have a lifetime of approximately 5000 hours, in comparison with a fuel cell engine where the lifetime is around 2000 hours. This problem occurs due to the frequent speed variations during car travel as the power consumption rises during the accelerations. If the speed were more or less constant the lifetime could be increased with a factor of 10 to 20. An application where the fuel cells have better lifetime is in CHP systems of hundreds of kilo watts. In these systems the changes in output power are small which gives a longer lifetime.

- Manufacturing and environment

Most people consider fuel cells to be an environmentally benign energy converter. That is true with some modifications. Depending on how the hydrogen fuel is produced the fuel is more or less carbon dioxide (CO2) free. If it is produced with green electricity, i.e., environmentally benign produced energy from renewable and non-polluting energy sources, the fuel is said to be clean. However, when the production uses electricity from fossil fuels such as coal, oil and natural gas there will be emissions to the atmosphere.

An aspect that is seldom thought of is the manufacture of the cell. The fact that the electrodes and electrolyte are made thin and that the electrode surfaces have a microstructure makes the manufacturing energy demanding. When the cells are bound together into a stack, bipolar plates could be used. These are made from good conducting materials such as graphite or stainless steel. The mining of the raw materials for the plates is energy demanding and gives air pollution and soil contamination. Another environmental problem is that platinum often is used as a catalyst for the electrodes. Platinum is a very scarce metal and when mining, the percentage of pure platinum is very low. This leads to many different processes which are both energy demanding and polluting.

- Advantages and Drawbacks

As all technical equipment fuel cells have both advantages and drawbacks. The different drawbacks are more or less important depending on the application and the economy of the project. A short summary of important advantages and drawbacks are listed below.

The advantages are:

· Low emissions

· More efficient compared to a conventional internal combustion engine

· Simplicity, few if any moving parts

· Reliable and long-lasting system

· Silent

The drawbacks are:

· Lifetime

· Cost

· Hydrogen has to be produced

· Not yet available infrastructure for hydrogen

- Components of PEMFC

A typical PEM element consists of several components.

First, there is a current collector.

Fig. 12: Current collector

Next, gas diffusion layer for anode (the gas diffusion layer consists of carbon fibers)

Fig. 13: Gas diffusion layer for anode

Then the membrane electrode assembly, which consists of anode and cathode catalysts deposited onto a nafion membrane (the electron microscopy shows that the cathode catalyst layer is much thicker than anode).

Fig. 14 : Membrane electrode assembly

Next , the cathode gas diffusion layer

Fig. 15: Cathode gas diffusion layer

A perforated metal plate

Fig. 16: Perforated metal plate

And finally the bipolar plate, which acts as a current collector and distributes air in the element.

Fig. 17: Bipolar plate

To create a working fuel cell stack, several single cells are connected in series.

Fig. 18: Single cell

Fig. 19: Stack of PEMFC

Fig. 20: Air inlet and cooling

- How Fuel Cells Work

Fig. 21: An exploded view of a fuel cell stack

Fig. 22: Basic micro fuel cell based upon traditional fuel cell design 5

Fig. 23: Generalized schematic of a single fuel cell

Fig. 24: Schematic of a PEM fuel cell stack 5

Fig. 25:A cross section of the PEM fuel cell. The unit cell is made of 7 layers which are made of different compositions of material providing the layers with different properties

Fuel cells work like batteries, but they do not run down or need recharging. They produce electricity and heat as long as fuel is supplied. A fuel cell consists of two electrodes—a negative electrode (or anode) and a positive electrode (or cathode)—sandwiched around an electrolyte. A fuel, such as hydrogen, is fed to the anode, and air is fed to the cathode. In a hydrogen fuel cell, a catalyst at the anode separates hydrogen molecules into protons and electrons, which take different paths to the cathode. The electrons go through an external circuit, creating a flow of electricity. The protons migrate through the electrolyte to the cathode, where they unite with oxygen and the electrons to produce water and heat. Learn more about:

- Parts of a fuel cell

- Fuel cell systems

- Types of fuel cells.

  - Parts of a fuel cell

Fig. 26: PEMFC – flowing path of fuel and air

Polymer electrolyte membrane (PEM) fuel cells are the current focus of research for fuel cell vehicle applications. PEM fuel cells are made from several layers of different materials. The main parts of a PEM fuel cell are described below.

The heart of a PEM fuel cell is the membrane electrode assembly (MEA), which includes the membrane, the catalyst layers, and gas diffusion layers (GDLs).

Hardware components used to incorporate an MEA into a fuel cell include gaskets, which provide a seal around the MEA to prevent leakage of gases, and bipolar plates, which are used to assemble individual PEM fuel cells into a fuel cell stack and provide channels for the gaseous fuel and air.

### Membrane Electrode Assembly

The membrane, catalyst layers (anode and cathode), and diffusion media together form the membrane electrode assembly (MEA) of a PEM fuel cell.

  - Polymer Electrolyte Membrane

The polymer electrolyte membrane, or PEM (also called a proton exchange membrane)—a specially treated material that looks something like ordinary kitchen plastic wrap—conducts only positively charged ions and blocks the electrons. The PEM is the key to the fuel cell technology; it must permit only the necessary ions to pass between the anode and cathode. Other substances passing through the electrolyte would disrupt the chemical reaction. For transportation applications, the membrane is very thin—in some cases under 20 microns.

  - Catalyst Layers

A layer of catalyst is added on both sides of the membrane—the anode layer on one side and the cathode layer on the other. Conventional catalyst layers include nanometer-sized particles of platinum dispersed on a high-surface-area carbon support. This supported platinum catalyst is mixed with an ion-conducting polymer (ionomer) and sandwiched between the membrane and the GDLs. On the anode side, the platinum catalyst enables hydrogen molecules to be split into protons and electrons. On the cathode side, the platinum catalyst enables oxygen reduction by reacting with the protons generated by the anode, producing water. The ionomer mixed into the catalyst layers allows the protons to travel through these layers.

  - Gas Diffusion Layers

The GDLs sit outside the catalyst layers and facilitate transport of reactants into the catalyst layer, as well as removal of product water. Each GDL is typically composed of a sheet of carbon paper in which the carbon fibers are partially coated with polytetrafluoroethylene (PTFE). Gases diffuse rapidly through the pores in the GDL. These pores are kept open by the hydrophobic PTFE, which prevents excessive water buildup. In many cases, the inner surface of the GDL is coated with a thin layer of high-surface-area carbon mixed with PTFE, called the microporous layer. The microporous layer can help adjust the balance between water retention (needed to maintain membrane conductivity) and water release (needed to keep the pores open so hydrogen and oxygen can diffuse into the electrodes).

### Hardware

The MEA is the part of the fuel cell where power is produced, but hardware components are required to enable effective MEA operation.

- Bipolar Plates

Each individual MEA produces less than 1 V under typical operating conditions, but most applications require higher voltages. Therefore, multiple MEAs are usually connected in series by stacking them on top of each other to provide a usable output voltage. Each cell in the stack is sandwiched between two bipolar plates to separate it from neighboring cells. These plates, which may be made of metal, carbon, or composites, provide electrical conduction between cells, as well as providing physical strength to the stack. The surfaces of the plates typically contain a “flow field,” which is a set of channels machined or stamped into the plate to allow gases to flow over the MEA. Additional channels inside each plate may be used to circulate a liquid coolant.

- Gaskets

Each MEA in a fuel cell stack is sandwiched between two bipolar plates, but gaskets must be added around the edges of the MEA to make a gas-tight seal. These gaskets are usually made of a rubbery polymer.

  - Fuel cell systems

The design of fuel cell systems is complex and can vary significantly depending upon fuel cell type and application. However, several basic components are found in many fuel cell systems:

- Fuel cell stack

- Fuel processor

- Power conditioners

- Air compressors

- Humidifiers.

### Fuel Cell Stack

The fuel cell stack is the heart of a fuel cell power system. It generates electricity in the form of direct current (DC) from electrochemical reactions that take place in the fuel cell. A single fuel cell produces less than 1 V, which is insufficient for most applications. Therefore, individual fuel cells are typically combined in series into a fuel cell stack. A typical fuel cell stack may consist of hundreds of fuel cells. The amount of power produced by a fuel cell depends upon several factors, such as fuel cell type, cell size, the temperature at which it operates, and the pressure of the gases supplied to the cell.

    - Fuel Processor

The fuel processor converts fuel into a form usable by the fuel cell. Depending on the fuel and type of fuel cell, the fuel processor can be a simple sorbent bed to remove impurities, or a combination of multiple reactors and sorbents.

### Power Conditioners

Power conditioning includes controlling current (amperes), voltage, frequency, and other characteristics of the electrical current to meet the needs of the application. Fuel cells produce electricity in the form of direct current (DC). In a DC circuit, electrons flow in only one direction. The electricity in your home and workplace is in the form of alternating current (AC), which flows in both directions on alternating cycles. If the fuel cell is used to power equipment that uses AC, the direct current will have to be converted to alternating current.

Both AC and DC power must be conditioned. Current inverters and conditioners adapt the electrical current from the fuel cell to suit the electrical needs of the application, whether it is a simple electrical motor or a complex utility power grid. Conversion and conditioning reduce system efficiency only slightly, around 2%–6%.

### Air Compressors

Fuel cell performance improves as the pressure of the reactant gases increases; therefore, many fuel cell systems include an air compressor, which raises the pressure of the inlet air to 2–4 times the ambient atmospheric pressure. For transportation applications, air compressors should have an efficiency of at least 75%. In some cases, an expander is also included to recover power from the high-pressure exhaust gases. Expander efficiency should be at least 80%.

### Humidifiers

The polymer electrolyte membrane at the heart of a PEM fuel cell does not work well when dry, so many fuel cell systems include a humidifier for the inlet air. Humidifiers usually consist of a thin membrane, which may be made of the same material as the PEM. By flowing dry inlet air on one side of the humidifier and wet exhaust air on the other side, the water produced by the fuel cell may be recycled to keep the PEM well hydrated.

- Cell structure

Fig. 27: Cell structure

We have here a half cell to represent is in a symmetrical structure although their function would be different so on each side, we will have what is called a bipolar plate, it is a plate which must lead, which must direct the gases in the channels. It must conduct electricity to collect electrons. It must make it possible to separate the hydrogen and the oxygen in order to avoid a possible explosion, it must allow the heat to be evacuated, it provides the mechanical support of the cell and it possibly makes it possible to evacuate gases, in particular from the gas. air which mainly exceeds nitrogen and water which is produced by the chemical reaction.

Then we have gaskets, gaskets are usually calcium or silicone, they are there only to avoid queues and hydrogen leakage is therefore a fuel cell explosion.

Then in the GDL of a gas diffuses the best therefore the diffusion layer which is generally a sheet or a carbon fabric for them which therefore catches the role of diffusing the gases on the whole of the catalytic layer to evacuate the water produced by the reaction. It must also conduct electricity must be made of carbon conduct heat to evacuate it and it provides a certain mechanical support which prevents the shape of the channels from destroying the membrane.

Then the catalytic layer which is formed of carbon on which their effects are the smaller platinum particles possibly mixing with a solution of Nafion. Nafion which is the solution which is used to produce the membrane so this catalytic layer and the sludge functions, it must allow the diffusion of gases that it can react, it must catalyze the reaction must allow proton to pass into the membrane. It must conduct electricity to the layers of the diffusions, it must have as large a surface area as possible to increase the power of our fuel cell at an equivalent volume, it must have the longest possible lifespan and we strive to make sure that it resists any form of imprisonment like carbon monoxide which can ruin fuel cells pretty fast.

Finally, we have the membrane which is made of a Nafion polymer containing the carboxylic ions with the same fluorine which has the property not to conduct electricity but to conduct protons which makes the reaction possible.

It must also ensure tightness so as to prevent hydrogen and oxygen from this mixture directly and causing an explosion.

Fig. 28: Structural setup

- Analysis of quantities

  - Fluidic quantities

    - In the canals

Fluidic quantities

- The gases have a pressure of 1 to 8 bars

- Hydrogen flow rate: 0.1e-3 mol / sec to 1000 mol / sec

- Air flow: 1E-3 to 1000 mol / sec.

Settings

- Channel length: 1 - 8 m

- Channel diameter: 0.1 to 5 mm

- Parallel number: 1 – 8

Pressure distributions (O2)                    	                    Dynamic

Fig. 29: Fluidic quantities (Pressure distributions & dynamics) variations in the canals

    - In the GDL

Sizes

- Pressure 1 - 2 bar

- Flow 0.1 - 1E-3 mol / sec

Setting

- Diffusion coefficient 2.5 - 9E-5

- Thickness of the scattering layer 0.2 - 0.6 mm

Distributions                                                 Dynamic

Fig. 30: Fluidic quantities (Distributions & dynamics) variations in the GDL

    - In the membrane

Sizes

- Water concentration: 0.001 to 0.2 mol / m3

Setting

- Thickness 150 - 400 μm

But we make membranes thinner and thinner as we can improve their existence in order to reduce losses by Joule effect

Distributions (liquid saturation)                                             Dynamic

Fig. 31:Fluidic quantities (Distributions & dynamics) variations in the membrane

  - Thermal quantities

    - In the electrode

Size

- Temperature: from 290 to 333 K (from 20˚C to 60˚C)

Settings

- Thermal conduction 175 W/K

- Thermal capacity 24 J/K

- In a commercial pile such as the harness ball that it takes 1 sec to cancel 7 K with cooling system

Distributions                                         Dynamic

Fig. 32: Thermal quantities (Distributions & dynamics) variations in the electrode

    - In the GDL membrane / catalytic layer assembly

Size

- Temperature

Settings

- Thermal capacity 4 J/k

- Conduction 11 w/k

- 0.3 sec/k for temperature stabilization

  - Electric dynamic

    - In the channels and the diffusion layer

Sizes

- Current: 0 - 50 A

- Voltage of a cell: 0.5 - 1.3 V

Setting

- Resistance of a cell: 15 μΩ

Distributions                                                  Dynamic

Fig. 33: Electric dynamic (Distributions & dynamics) variations in the channel & the diffusion layer

    - In the catalytic layer

Sizes

- Voltage of one cell 0.5 - 1.3 v

- Current 0 - 50 A

Setting

- Double layer capacitance 2 - 3 F

    - In the membrane

Sizes

- Voltage 0.5 - 1.3 v

- Current 0 - 50 A

Setting

- Resistance 0.25 – 3 Ω

Distributions (water content)                                      Dynamic

Fig. 34: Electric dynamic (Distributions & dynamics) variations in the membrane

- Parametric influence

  - In the canals

A change in pressure has very little influence on heat and vice versa, and the device has relatively little input between heat and electric current and between electric current and movement. on the other hand, one can have an acceleration of 1.5 mm/sec per additional year pair in a conventional pile. Same in the diffusion layer.

Same in the diffusion layer                                    In the diffusion layer

Fig. 35: Parametric influence in the canal

  - In the catalytic layer

In the catalytic layer, 30% variation in attention for 100% variation in temperature so we still had an influence which can be significant between the temperature and the voltage which is linked to the losses. function the temperature we have not the same allowed the same result with the berne law is not to mention the effect of the temperature under the fuel cell the voltage little increased by 25% for an oxygen concentration 10% higher therefore also for strong currents. if we have an agreement between the oxygen concentration which decreases we have a significant loss of tension a temperature increase of 10 degrees in the membrane can multiply its electrical resistance by 3 and the influence of water it is also very important therefore we can divide by three the resistance for a concentration of other two times higher and when we have 75% we can still reduce the resistance by 30% so water is very important in the limbs there.

Fig. 36: Parametric influence in the catalytic layer

  - In the membrane

An increase in temperature of 10 degrees in the membrane can multiply its electrical resistance by three and the influence of water is also very important so we can divide by three the resistance for a concentration of other two times higher and when we at 75% we can further reduce the resistance by 30% so water is very important in the membrane there.

Fig. 37: Parametric influence in the membrane

- Comparison of Fuel Cell technologies

Fig. 38: Comparison of Fuel Cell technologies

Fig. 39: Comparison of Fuel Cell type

- Production process of PEM fuel cell components

● Due to the small production volumes of fuel cells, there is currently no
generally valid process chain for the series production of PEM fuel cell
components.
● Production of a PEM fuel cell system can be divided into three superordinate steps: component production, stack production and system production.
● This brochure presents the process steps that constitute the current state of the art in the production of PEM fuel cell components.
● Production of the fuel cell stack and system is explained in more detail in a separate brochure entitled "Production of Fuel Cell Systems”.

Component Production:

Fig. 40: Production process of PEM fuel cell components

- Overview of PEM fuel cell components

Fig. 41: Overview of catalyst coated membrane

Fig. 42: Overview of Gas diffusion layer (GDL)

Fig. 43: Overview of bipolar plate

- Thermal Engineering Performance Evaluation of a Polymer Electrolyte Membrane Fuel Cell Stack at Partial Load

  - Thermal Engineering Analysis

Stack heat generation is a theoretical heat quantity based on the conversion efficiency of the fuel cells. The theoretical maximum voltage for a single cell based on the Higher Heating Value of hydrogen is 1.482 V when the products are all in liquid state. The stack for this work has a design rating of 45% efficiency at full load, and the theoretical heat generation for the stack can be estimated using Equation (6).

(6)

In equation (6), I represent the stack current in Ampere (A) and ncell is the number of cells of the stack.

Equations 7 to 19 are applied accordingly for the analysis where the scope covers the relation of stack thermal conditions to output power, active-to-passive cooling contributions, and cooling system effectiveness.

The electrical power output in Watts,

(7)

For a single cell, the cell efficiency

(8)

Thus, the stack efficiency was evaluated using

(9)

The cooling mechanism of the fuel cell stack is categorized as active cooling and passive cooling. Active cooling is achieved by circulating cooling water internally and using an air-cooled heat exchanger (radiator) to dissipate the heat to the surrounding. Active cooling theoretically contributes at least 90% [12] of the total cooling effect. Passive cooling plays only a minor role, but the effects are more significant as the stack temperature increases.

The calculation of active cooling rate is based on the energy property changes of the cooling water as it carries away the heat from the fuel cell stack.

Cooling water energy changes,

(10)

Air energy changes,

(11)

The subscripts cw and a are for cooling water and air respectively, while subscripts e is for the exit state and i for the inlet state. The net heat in the stack related to the temperature difference over a certain time period,

(12)

Passive cooling over the exposed stack surfaces consists of free (natural) convection by the ambient surroundings as well as heat transfer by radiation. The free convection cooling effect is based on

(13)

In this case, the surface areas involved are two vertical flat side surfaces, two vertical flat end surfaces, and one horizontal surface with heated surface facing upward. The Nusselt number correlations were calculated for each orientation and the respective free convection coefficient, h, and surface cooling is calculated.

Cooling by radiation heat transfer is expressed by

(14)

σ is the Stefan-Boltzmann constant, equals to 5.67 x 10-8, and ε is the surface emissivity.

Thus, the passive cooling rate is the summation of free convection and radiative cooling over the stack surfaces,

(15)

The total cooling effect is the summation of active and passive cooling rates.

(16)

From equations (7) and (11), the total stack thermal power can be calculated.

(17)

For the radiator, the analysis on the radiator effectiveness is evaluated by,

(18)

The maximum possible cooling rate in a heat exchanger is

(19)

where Cmin is the smaller of  and .

  - Experimental Method

The experiment was conducted using a PEM fuel cell system designed for Uninterrupted Power Supply (UPS). The system configuration and general specifications of the hardware are presented in Figure 44 & 45 respectively. The working fluids are hydrogen, reactant air, cooling water and cooling air. Figure 46 summarizes the operating conditions of the experimental. The measurements were taken at 3 minutes intervals using a thermal scanner and K-type thermocouples with data logger for local temperatures at 18 designated points of the stack, anemometer for air velocity and temperature, and a multi-meter for electrical power measurement at the resistant loader.

Fig. 44: PEM fuel cell system specifications

Fig. 45:  Operating conditions of fuel cell

Fig. 46: The fuel cell system schematic

Fig. 47: Relation of stack temperature to electrical power

Fig. 48:The total stack thermal energy compared to combined cooling effects

Fig. 49: Relation of stack heat and stack-to-cooling water temperature profile

Fig. 50: Active and passive cooling contribution percentages

Fig. 51: Theoretical optimum cooling contributions of passive and active cooling

  - Cooling Performance

Fig. 52: Temperature profile at heat exchanger

Fig. 53: Effectiveness of the heat exchanger at steady-state

  - Conclusions

Experimental analysis of a water-cooled PEM fuel cell system shows that the stack temperature can be largely influenced by the coolant. The stack temperature increased to unacceptable levels due to the influence from the cooling water temperature. To maintain the stack at the required operating temperature below 50˚C, the generated heat needs to be adequately dissipated by an active cooling system operating higher than 90% cooling effectiveness, and the cooling water temperature at the inlet and outlets of the stack must also be controlled below 40˚C at all times. With a registered effectiveness of less than 50%, unsuitable operating conditions of the heat exchanger was identified as the main cause for the thermal problem facing the stack, especially regarding the flow rates of both fluids.

- Consideration for Fuel Cell Design

When you first consider your fuel cell stack design, you will need to calculate the following:

• Stack size
• Number of cells (MEAs / CCMs)
• Stack configuration (flow field plates, GDL, etc.)

This paragraph presents an overview of the initial considerations for fuel cell design in room-temperature fuel cells.

## Fuel Cell Stack Size

The first step in engineering a fuel cell stack is to obtain the power requirements. The stack is then designed to meet those requirements, and the maximum power, voltage, and current are often known. The power output of a fuel cell stack is a product of stack voltage and current:

(20)

The maximum power and voltage requirements are dependent upon the application. The engineer must understand these specifications to build an appropriately-sized fuel cell stack. It is helpful to know the current and power density when designing a fuel cell stack. These are often unavailable initially but can be calculated from the desired power output, stack voltage, efficiency, and volume and weight limitations. The current is a product of the current density and the cell active area:

(21)

The cell potential and the current density are related by the polarization curve:

(22)

An example of a polarization curve is shown in Figure below. The polarization curve can be used to help initially design the fuel cell stack.

Fig. 54: Typical polarization curve for a PEM fuel cell stack.

Most fuel cell developers use a nominal voltage of 0.6 to 0.7 V at nominal power. Fuel cell systems can be designed at nominal voltages of 0.8 V per cell or higher if the correct design, materials, operating conditions, balance-of-plant, and electronics are selected.

The actual fuel cell performance is determined by the pressure, temperature, and humidity based on the application requirements, and can often be improved (depending upon fuel cell type) by increasing the temperature, pressure, and humidity, and optimizing other important fuel cell variables. The ability to increase these variables is application-dependent because system issues, weight, and cost play important factors when optimizing certain parameters.

## Number of Cells

The number of cells in the stack is often determined by the maximum voltage requirement and the desired operating voltage. The total stack potential is the sum of the stack voltages or the product of the average cell potential and number of cells in the stack:

(23)

The cell area must be designed to obtain the required current for the stack. When this is multiplied by the total stack voltage, the maximum power requirement for the stack must be obtained. Most fuel cell stacks have the cells connected in series, but stacks can be designed in parallel to increase the total output current. When considering the stack design, it is preferable to not have cells with a small or very large active area because the cells can result in resistive losses. With fuel cells that have large active areas, it can be difficult to achieve uniform temperature, humidity and water management conditions.

The cell voltage and current density is the operating point at nominal power output and can be selected at any point on the polarization curve. The average voltage and corresponding current density selected can have a large impact on stack size and efficiency. A higher cell voltage means better cell efficiency, and this can result from the MEA materials, flow channel design, and optimization of system temperature, heat, humidity, pressure, and reactant flow rates. The fuel cell stack efficiency can be approximated with the following equation:

(24)

## Stack Configuration

In the traditional bipolar stack design, the fuel cell stack has many cells stacked together so that the cathode of one cell is connected to the anode of the next cell. The main components of the fuel cell stack are the membrane electrode assemblies (MEAs), gaskets, bipolar plates with electrical connections and end plates. The stack is connected by bolts, rods, or other methods to clamp the cells together.

When contemplating the appropriate fuel cell design, the following should be considered:

• Fuel and oxidant should be uniformly distributed through each cell, and across their surface area.
• The temperature must be uniform throughout the stack.
• If designing a fuel cell with a polymer electrolyte, the membrane must not dry out or become flooded with water.
• The resistive losses should be kept to a minimum.
• The stack must be properly sealed to ensure no gas leakage.
• The stack must be sturdy and able to withstand the necessary environments.

The most common fuel cell configuration is shown in Figure 2. Each cell (MEA) is separated by a plate with flow fields on both sides to distribute the fuel and oxidant. The fuel cell stack end plates have only a single-sided flow field. Most fuel cell stacks, regardless of fuel cell type, size and fuels used are of this configuration.

Fig. 55: Typical fuel cell stack configuration (a two-cell stack)

# Polymer Electrolyte Membrane Fuel Cells (PEMFCs)

The polymer electrolyte (also called proton exchange membrane or PEM) fuel cell delivers high-power density while providing low weight, cost, and volume. A PEM fuel cell consists of a negatively charged electrode (anode), a positively charged electrode (cathode), and an electrolyte membrane, as shown in Figure 56. Hydrogen is oxidized on the anode and oxygen is reduced on the cathode. Protons are transported from the anode to the cathode through the electrolyte membrane and the electrons are carried over an external circuit load. On the cathode, oxygen reacts with protons and electrons forming water and producing heat.

In the PEM fuel cell, transport from the fuel flow channels to the electrode takes place through an electrically conductive carbon paper, which covers the electrolyte on both sides. These backing layers typically have a porosity of 0.3 to 0.8 and serve the purpose of transporting the reactants and products to and from the bipolar plates to the reaction site [1]. An electrochemical oxidation reaction at the anode produces electrons that flow through the bipolar plate/cell interconnect to the external circuit, while the ions pass through the electrolyte to the opposing

4

Fig. 56: Physical characters of proton exchange membrane fuel cell (PEMFC)

Fig. 57: The polymer electrolyte fuel cell (PEMFC) 4

electrode. The electrons return from the external circuit, while the ions pass through the electrolyte to the opposing electrode. The electrons return from the external circuit to participate in the electrochemical reduction reaction at the cathode. The reactions at the electrode are

The standard electrolyte material currently used in PEM fuel cells is a fully fluorinated Teflon-based material produced by DuPont for space applications in the 1960s. The DuPont electrolytes have the generic brand name Nafion, and the types used most frequently are 1135, 115, and 117. The Nafion membranes are fully fluorinated polymers that have very high chemical and thermal stability. The electrodes are thin films that are bonded to the membrane. Electrodes with low platinum loading perform as well or better than high-platinumloaded electrodes. To improve the utilization of platinum, a soluble form of the polymer is incorporated into the porosity of the carbon support structure. This increases the interface between the electrocatalyst and the solid polymer electrolyte [2].

  - Basic stationary fuel cell calculations.

In order to evaluate and compare stationary fuel cell systems, the following efficiencies can be calculated for all of the components and aspects of the fuel cell system. The total efficiency of the fuel cell system is defined as:

Total efficiency = (electric power output + thermal output) / fuel consumption                                                                  (25)

Or                                                                      (26)

where Pnet, and Qnet is the usable power and heat amounts respectively, and

nfuel is the amount of fuel input into the fuel cell system. The total efficiency

of the fuel cell system can also be calculated by multiplying the efficiencies

of the individual components, and the ratio of parasitic power and fuel cell

gross power output (ξp). An example of this equation is as follows:

(27)

The electrical efficiency of the stationary fuel system is:

(28)

Where                                                         (29)

And                     (30)

where PAC is the usable AC power generated, Paux_equipment is the power required by auxiliary equipment, Pcompressor is the power required by compressor, Ppump is the power required by the pump, and Pcontrol is the power required by the control system.

The thermal efficiency of the stationary fuel cell system is:

(31)

If the stationary fuel cell system uses a fuel processor, the efficiency of the fuel processor is:

(32)

The DC/AC efficiency of the stationary fuel cell system is:

(33)

For any auxiliary equipment used, the efficiency is:

(34)

The efficiency of the fuel cell stack is:

(35)

  - Fuel Cell Reversible and Net Output Voltage

The maximum electrical energy output, and the potential difference between the cathode and anode is achieved when the fuel cell is operated under the thermodynamically reversible condition. This maximum possible cell potential is the reversible cell potential. The net output voltage of a fuel cell at a certain current density is the reversible cell potential minus the irreversible potential which is discussed in this section, and can be written as [3]:

(36)

where Vrev = Er is the maximum (reversible) voltage of the fuel cell, and Virrev is the irreversible voltage loss (overpotential) occurring at the cell.

The maximum electrical work (Welec) a system can perform at a constant temperature and pressure process is given by the negative change in Gibbs free energy change (ΔG) for the process. This equation in molar quantities is:

(37)

The Gibbs free energy represents the net energy cost for a system created at a constant temperature with a negligible volume, minus the energy from the environment due to heat transfer. This equation is valid at any constant temperature and pressure for most fuel cell systems. From the second law of thermodynamics, the maximum useful work (change in free energy) can be obtained when a “perfect” fuel cell operating irreversibly is dependent upon temperature. Thus, Welec, the electrical power output is:

(38)

where G is the Gibbs free energy, H is the heat content (enthalpy of formation), T is the absolute temperature, and S is entropy. Both reaction enthalpy and entropy are also dependent upon the temperature. The absolute enthalpy can be determined by the system temperature and pressure and is usually defined as combining both chemical and thermal bond energy. The change in the enthalpy of formation for the chemical process can be expressed from the heat and mass balance:

(39)

where  the summation of the mass times the enthalpy of each substance leaving the system, and  is the summation of the mass times the enthalpy of each substance entering the system. Asimple diagram of the heat and mass balance is shown in Figure below.

The potential of a system to perform electrical work by a charge, Q (coulombs) through an electrical potential difference, E in volts is [4]:

(40)

If the charge is assumed to be carried out by electrons:

(41)

Fig. 58: Fuel cell heat and mass balance

Fig. 59: Simple PEM fuel cell system [5]

- Model creation of PEM fuel cell

Fig. 60: Dimensions of PEM fuel cell model

Fig. 61: Model of serpentine channel flow field of PEM fuel cell

Fig. 62: The analysis was done with three different pressure (1 bar, 1.5 bar, 2 bar) and voltage (0.25 V-0.85 V) at constant temperature of 323 K (50oc) using Ansys and checked

  - Material and assembly (exp)

Table below summarises the material properties of the fuel cell components used in this study and Fig below shows the assembly steps of the PEM fuel cell. The optimised OPCF flow plate housing was machined and wiped thoroughly using isopropyl alcohol to ensure that the housing is clean and no dust or grease present. The flow plate housing is placed horizontally in a flat position. OPCF was polished using silicon carbide grinding paper on a polishing wheel. The OPCMF is placed inside the housing and bolts are placed through the housing as shown in Fig below, photo 2. A gasket is then placed into position as shown in Fig below, photo 3. The MEA is positioned onto the housing as shown in Fig below, photo 4. A second gasket is then placed onto the MEA as shown in Fig below, photo 5. A second OPCF flow plate is placed into a second housing as shown in Fig below, photo 6. The second housing is then placed onto the bolts of the first housing. The MEA and gasket positions are checked and both housings are closed. Nuts are placed on the bolts and they are tightened. The push-in fittings for hydrogen pipes are placed in their positions. The final assemble fuel cell is shown in Fig below, photo 7.

Fig. 63: Assembly steps of the PEM fuel cell

Fig. 64: Material properties of the fuel cell component

  - Experimental set-up and procedure 14

The experimental setup is similar to Carton & Olab [6]. The reactant gas, hydrogen, is stored in a compressed cylinder. A specialized hydrogen pressure controls the hydrogen gas flow pressure. The gas then passes through volumetric flow meters. The flow controllers are calibrated for the hydrogen gas and air. The flow controllers are controlled by the data acquisition (DAQ) software (Lab View). Both air and hydrogen gases were humidified as stated by the manufacturer of the MEA. The open circuit voltage and the fuel cell operating voltage are detected by the DAQ hardware and analyzed through the software. The open circuit voltage reading is also double checked at the anode and cathode using a multi-meter (Fluke 8808A digital multi-meter). The fuel cell current is measured using a multi-meter (Fluke 8808A digital multi-meter) in series with the external load.

Every effort was made to keep parameters constant during the experiments to ensure that the values of resistance, pressure and flow were not changed from one experiment to the next. These parameters were checked throughout the experiment to identify any unwanted errors. The only effect on the performance was that of the flow plate design.

Fig. 65: The Polymer Electrolyte Membrane Fuel Cell (PEMFC)

Fig. 66: Schematic of Polymer Electrolyte Membrane Fuel Cell showing different components

Fig. 67: Condensation of water produced by a PEMFC on the air channel wall. The gold wire around the cell ensures the collection of electric current

- Study of PEM Fuel Cell End Plate Design by Structural Analysis Based on Contact Pressure

  - Introduction

Polymer electrolyte membrane fuel cell (PEMFC) is one of the promising technologies for electrical power generation. Presently, PEMFCs utilize solid polymer membrane as an electrolyte and porous carbon cloth/paper as electrode. The electrode and electrolyte together are referred to as the membrane electrode assembly (MEA) which is equipped with bipolar plate (BPP) on both the sides for reactant flow and current collection. A number of such units (single cells) are connected in series and are flanked by endplate at both ends to form a fuel cell stack. Graphite is usually the material of choice for bipolar plates due to its high corrosion resistance but still lighter material is preferred for the endplate [7, 8]. PEMFC has received considerable attention, especially in the automotive sector as the low operating temperature (< 100°C) allows quick start-up and portability [9, 10].

  - Description of Geometry

The geometry considered in the simulation includes the end plates, two bipolar plates, two gaskets, two GDLs, and a membrane. GDLs are joined to the membrane as nonseparable entities. As in common assembly procedure, the membrane is placed in the middle, with GDL on each side, followed by the gasket. This assembly is sandwiched between the bipolar plates and is enclosed by the end plates as shown in Figure above. In the geometry analysis ten bolts are considered with two configurations, one is with all bolts outside the graphite plates and the other one is with all bolts inside the graphite plates.

Fig. 68: Schematic geometry of PEMFC

Fig. 69: Material properties of PEMFC components

Geometries have been created in SOLIDWORKS and are imported in ANSYS® Academic Research, Release 14.0 workbench. Materials assigned are as shown in the Table 1. The flow channels of the bipolar plate are not included. Gasket material is selected as PTFE. GDL material is selected as carbon paper as it gives good performance due to high porosity (>70%) [6]. The clamping bolts considered are supposed to have standard M10 specifications. While evaluating the geometries, only the change in its external shape is considered, the total physical volume of the plate being kept constant. Reference end plate for the study is as depicted in Figure below.

Case 1 (evaluation of geometry). The size of end plate in our study is 300x200 mm2. Graphite plate, gasket, membrane, and current collector are each of dimension 267 × 172 mm2. Active area for all geometries is constant and it is equal to 199x154 mm2. All design features on end plates have same height of extrusion or cut 2 mm.

Case 2 (effect of number of bolts and position and its effect on contact pressure distribution). After obtaining the results of Case 1, the selected geometry is subjected to analysis in order to determine the effect bolt number and their arrangement.

For each of these schemes, the spacing between the adjacent bolts for each side of the end plate is given by

d = Ln+1

where “d” is the distance between adjacent bolts, “L” is the edge length, and n is the number of bolts.

Case 3 (analysis of pressure distribution considering that the bolt passes through the bipolar plate). After completing the analysis in Cases 1 and 2, the geometry and number and bolts are selected. The bolt position is then shifted such that it lies inside the bipolar plate and the change in pressure distribution is determined.

Case 4 (evaluation of the effect of gasket thickness). In most of the previous studies, the BPP is assumed to be in perfect contact with GDL while performing the FEA. However, in most practical scenarios, there is some difference between the gasket and GDL thickness. This mismatch produces an initial no-contact region between BPP and GDL, when compressive forces are gradually applied.

The final geometry obtained after three successive case studies is subjected to further analysis for evaluating the effect of change in the gasket thickness. Gasket thickness is changed in three equal steps from 0.1 to 0.2 mm, keeping the thickness of GDL constant (0.4mm).

Case 5 (evaluation of different end plate materials). The influence of the end plate material on the pressure distribution, stresses, and deformation is investigated using different materials. It is implemented using the configuration chosen after analysing the result of the previous cases.

  - Boundary condition

The current study shall act as a guideline for future fuel cell design activities, since it provides a comprehensive solution for ensuring homogeneous pressure distribution, leakage proof operation, and improving performance.

Several end plate geometries were considered in this study, along with number of bolts used in tightening and their position with respect to the cell. Extruded hexagonal geometry for end plate shows better distribution of contact pressure. Number of bolts is found to have a significant impact on average contact pressure and distribution. In the study, it is found that 10 bolts are suitable for obtaining uniformity for the structure under study. Bolt placement also has a considerable impact on the average contact pressure and contact pressure distribution, i.e., by placing all bolts through the graphite plate has contributed to more uniform contact pressure distribution.

Another important aspect of cell assembly is to choose a gasket thickness complementary to thickness of the GDL for a given compressive pressure. The evaluations of gasket thickness from this study shall provide insights into the permissible gasket thickness. It is found that the difference between GDL and gasket is tolerable between 0.15 mm to 0.2mm. Thus, by optimizing geometry, number of bolts, their position, and gasket thickness, average contact pressure of ~ 0.8 MPa is obtained at a bolt loading of 8–10 Nm. Change in material is found to be of lesser importance. However, lighter materials like aluminium alloys can be effectively utilized, producing weight savings of ~65% while retaining better contact pressure distribution.

- Components in a single cell

The figure above shows the expansion diagram of a single cell. Inside the single cell, we can see the first of course the MEA which had a no catalyst layer Castle Caturday, and separator which is a counter ionic conductive but electronically is insulate. And next to the MEA is the TDA of gaskets if you layer will be mentioned them. Since the it had to be carried transport the gas in and out so it’s a porous medium and even the outside the oscar of the is also porous so the gas will leak out from the outside here so we need the gasket to prevent gas leakage, and the gas key is made of flexible Teflon, so it’s a chemical inner but also still the guest so that will not let the gas leak of an outside and also acting as a insulation.

Then we call the graphite plate. The graphite plate actually might be the graphite powder or carbon powder mixed with phenolic resin and compressed into a plate and the under surface of the play had a curve into the flow channel so the reactant the guest will be when a flow through the channel will be able to evenly distribute through the GDL to the electrode surface and also the current or electron generation.

And know we flow out through the GDL and to the graphite plate. Because the disk graphite plate is in touch with korg component for the sphere cell is maybe corrosive so it’s had to be used carbon material to make sure it’s when a corrode and but also the current and outside will be the current collector, the current carried out by the current collector an outer cell. The reason we had to need a current collector is the electronic conductivity of the current collector is a more than a thousand times higher than the graphite plate. This current quality usually made of copper maybe but usually is highly electronic conductive but because we use a graphite plate to insolate to prevent any corrosive gas or the environment so they will be not corroded but this will very highly conductive so the current can be disputed evenly through th egraphite plate to the GDL and then we had end plate. The purpule for the end plate is try to contact or transmit the screw pressure even into the center because the channel graphite plate.

The channel plate and then GDL and the electro here need a pressure to compress together to reduce possible interfacial resistance electronically distance between a graphite plate or GDL to the catalyst layer. You need a pressure to press down to reduce the individual pressure but you cannot punch a hole and make a school to tight it up so you had to add a screw tigher on the periphery of the graphite plate to this one had to enough pressure to press on the GDL. So this end plate have a stick and then will become complete the screw pressure to the center even a dispute so that said understand the pressure can be evenly compressed. There’s a basic a key component for a single cell that for the MEA the GDL cascade graphite plate current collector and end plate.

Fig. 70: Components in a single cell

- Fuel cell stack

  - Add cell to the stack

Form the anode’s side                                           From the cathode’s side

Fig. 71: Stack of the PEMFC from the anode & cathode side

We have 5 cells in our hydrogen fuel cell. To add 2 cells to the fuel cell, you must first remove the bolts and nuts

Fig. 72: Remove the bolts and nuts from stack

Then we remove the end plate

Fig. 73: Remove the end plate from the stack

Then we remove the current plate collector, with the gasket

Fig. 74: Remove the current plate collector, with the gasket from the stack

This is what we have. It's the first cell next to the current collector. We can see there is a channel. And this channel is the liquid cooling add in the end plate

Fig. 75: First cell next to the current collector

For more details, we will review the details of a single cell. These is the cell itself, so that the components required for single cell. Two graphite plate and one membrane electrode assembly (MEA).

Fig. 76: Overview of a single cell (Two graphite plate and one MEA)

We can see the gasket layers and the subgasket use two support the electrolytic membrane

Fig. 77: The MEA layer

Each plate equiped with the single gasket and the gas distribution channel with multiple support flow field, and field gasket and in the middle holes to field the liquid cool.

Fig. 78: Gas distribution channel with multiple support flow field, and field gasket at the front side

We turn the plate, we can see the hole is connected through the plate.

Fig. 79: Gas distribution channel with multiple support flow field, and field gasket at the back side

Basicly, how it is made very simple. One plate, from the channel side, one MEA placed on the plate with gasket and the another plate ,with gasket, puted on the MEA like this. And we have like one cell.

Fig. 80: Steps to build a cell

And now, we want to add this cell to the rest of the stack

I will first take this plate. We will start with this plate because it is flush. If we have like this gasket is here and cooling channel is here so we will place plate flush.

Fig. 81: Add the plate in the appropriate direction to the stack

Add the gasket

Fig. 82: Add the gasket

Now we added the MEA

Fig. 83: Add the MEA

And add the gasket

Fig. 84: Add the second gasket

And emplacing the plate through the tie rod.

Fig. 85: Emplacing the plate through the tie rod

I will now move to add the second cell. I want to add to the stack the cell. we seen before is ready with MEA inside. And this cell is equiped with cooling channel on both side. For a simple reason, the last cell is flush so one cooling channel between the two half plate here and because it will be the last cell in the stack, there is also the cooling channel had is trun the side of the cell

Fig. 86: Add the second cell

Now what i need is again the current collector. We placed back.

Fig. 87: Placed back the current collector

And go nicely to placed the end plate

Fig. 88: Placed back the end plate

  - Working prototype

How to make a working prototype of such a do-it-yourself hydrogen fuel cell.

To do that, first, we need to make a platinum electrode we’ll use for oxidizing hydrogen and generating electricity . Metallic platinum is a great catalyst, which means it increases the rate of chemical reactions for instance. Since pure platinum is too expensive, to make electrdes from a thin platinum film on the surface of another metal will suffice for my experiment.

I am using such a nickel sponge sheet as a base for my platinum electrode, because Platinum coats this metal quite smoothly and without coming off. It besides because of this spanish sporus structure the surface area is maximized and the obtained catalyst will be extermely effective. Before going platinum plating, we need to remove grease and prepare the surface of the nickel sheet which is why first a large strips of the nickel sponge into an ultrasonic cleaner filled with soap solution. After cleaning nickel for 10 minutes i’m lowering these strips of nickel into a 50 alcohol solution in order to remove vestiges of soap and dirt. When running ultrasonic cleaning cavitation bubbles been released make sure that other dirt is removed from the pores of the nickel sponge. When the strips dried i got two clean electrodes.

Next for coating the nickel electrode with platinum, i’m using a quite expensive chemical called chloroplatinic acid costing 19 euros because this substance easily absorbs moisture from the air and melts. It is stored in sealed ampoules we’ll need an extremely weak solution of this substance, Just seven millimole per liter. First of all, i’m dissolving one gram of cloroplatinic acid in 15 mL of water, fortunately this chemical dissolves very well in water. and after that, i am pouring 9 grs of this solution into another beaker increasing the volume of the solution to 200 mL.

Now, i am lowering a pretty expensive and durable titanium electrode covered in irridium and russinium oxides into the obtained light yellowish solution such electrodes are used in gold and rhodium plating in order for the reaction to run more smoothly and for the solution not to get tainted in such an aggressive medium by the disintegrating anode.

To do platinum plating, i’m allowing a purified nickel sponge into the solution and starting to run electricity through it using my laboratory adapter during this process. Platinum is slowly covering the surface of nickel creating a very thin gray layer because of its slightly grainy structure it took me 20 minutes to cover one electrode with patinum. After that, i’m lowering it into distilled water in order to rinse off vestiges of the electrolyte. In some time, i got such two platinum electrodes for hydrogen batteries of quite good quality the dark areas are completely covered in pure platinum.

The next stage is making a case a hydrogen fuel cell, which i am going to make from two syringe cases. To increase their efficiency i have attached two valves to them which in the future will help me to run oxygen and hydrogen through my setup more smoothly. Now, i’m solderimg one platinum plated electrode to each syringe case using epoxy raisin on top of which i’m going to run chemical reactions.

This seemingly unremarkable film called nafion is the most important components of my hydrogen battery. They are sold as sandwiches in between two protective plastic layers. If we take a look at its chemical structure, from a chemical point of view it resembles teflon which is used to cover frying pans. The difference through is that several sulfur groups are added to the teflon skeleton enabling such a film to pass protons through it, which are hydrogen ions.

after separating nafion film from the protective plastic layer, It needs to be sandwiched in between the syringe cases, which i am also going to glue together the epoxy raisin hardens in 30 minutes. and after that, we can test my do-it-yourself hydrogen fuel cell for the first test.

I’m going to use a balloon filled with hydrogen. Then using a special burner, i began to supply halogen into the lower part of my setup, because these guys is lighter than air and it will be rising up towards the platinum catalyst. The upper syringe case will be filled with just air 20% of which is oxygen and i think it will be enough for my experiment as i start supplying hydrogen.

We can notice that the multimeter shows how the voltage is beginning to increase and it means that my setup works in some time the voltage reached 0.7 volt and remains more or less stable at this level. When i supply air through the upper part of the cell. The voltage slightly changes but not for long. So, what is happening here and how does this hydrogen fuel cell work.

To explain in simple terms, electricity in my cell is generated in the very middle at the interface of the two platinum electrons upon closing of the circuit when hydrogen is streamed into the lower part of the setup towards the surface of the lower platinum electrode. It gives off its electron which runs through the wire. The ion of hydrogen being created, or in other words proton which passes through that very naphthene film and ends up on the upper electrode there it is oxidized by the oxygen in the ear and receives the electron from the other electrode creating water.

As a result the lower electrode is negative or is an anode and the upper electrode is positive or in other words is cathode. in some time, there even condensed some water on the upper part of my setup which is a main by-product of this battery. My cell generates 0.7 V out of 1.3 theoretically possible. However the intensity of current isn’t very high being just 15 mA that is why unfortunately i won’t be able to connect anything to my hydrogen battery. The only way to increase the energy conversion efficiency of my battery is to make a more concentrated source of hydrogen.

For instanc to use sodium borohydride solution instead this compound can frequently be encountered at organic synthesis laboratoires, it is often used for reducing organic compounds because sodium borohydride easily gives off its hydrogen. It does is so easily than when dissolved in water. We can even see how bubbles are gradually being released from the sodium borohydride solution because this chemical isn’t stable in water and quickly breaks down.

If i turn my setup upside down and pour some sodium borohydrides into the upper part of the cell. I’ll immediately see how the multi-meter detects an increase in the voltage because in this case i am pouring concentrated hydrogen. Alright on the electrode thus, i can achieve high efficiency of my do-it-yourself hydrogen fuel cell having reached the maximum possible voltage. Unfortunately through not even sodium borohydride can increase the intensity of the electric current because my battery is too primitive because i cannot make a more efficient and beautiful fuel cell to continue my experiments.

- Fuel Cell Materials

  - Electrolyte Layer

Fig. 89: Common Materials Used for Each Fuel Cell Type

Fig. 90: Cation Exchange Membrane Comparison Chart

  - Fuel Cell Electrode Layers - PEMFC catalysts

Fig. 91: Anode catalyst materials

  - PEMFC gas diffusion layers

The gas diffusion layer is between the catalyst layer and the bipolar plates. In a PEMFC, the fuel cell layers (MEA) are sandwiched between flow field plates. On each side of the catalyst layer, there are gas diffusion backings. They provide electrical contact between the electrodes and the bipolar plates, and distribute reactants to the electrodes. They also allow reaction product water to exit the electrode surface and permit the passage of water between the electrodes and the flow channels.

Gas diffusion backings are made of a porous, electrically conductive material (usually carbon cloth or carbon paper). An illustration of carbon cloth and Toray paper is shown in Figure below. The substrate can be treated with a fluoropolymer and carbon black to improve water management and electrical properties. These material types promote effective diffusion of the reactant gases to the membrane/electrode assembly. The structure allows the gas to spread out as it diffuses to maximize the contact surface area of the catalyzed membrane. The thicknesses of various gas diffusion materials vary between 0.0017 to 0.04 cm, density varies between 0.21 to 0.73 g/cm2, and the porosity varies between 70 and 80 percent.

The GDL also helps with managing water in PEMFCs because it only allows an appropriate amount of water vapor to contact the membrane electrode assembly to keep the membrane humidified. In addition, it promotes the exit of liquid water from the cathode to help eliminate flooding. This layer is typically wet-proofed to ensure the pores in the carbon cloth or paper do not become clogged with water. The most common wet-proofing agent is PTFE.

Fig. 92: Carbon cloth and toray paper ( picture courtesy of Fuel Cell Scientific )

Fig. 93: Properties of Commercially Available Carbon Papers Used as Substrates In PEMFC Electrodes

- Constructing the Fuel Cell Bipolar Plates, Gaskets, End Plates, and Current Collectors

  - Bipolar plate design

Fig. 94: Properties of various types of bipolar plates for PEM fuel cells

Fig. 95: Process Options for Bipolar Plates

Fig. 96: Bipolar plate design for hydrogen and air flow channels for a PEMFC

  - Gasket selection

For the small air-breathing stack 0.010 or 0.020-inch silicone gaskets can be used (depending upon the fuel cell [MEA] thickness). Another popular option is using a 0.010-inch thick fiberglass reinforced silicone rubber anode gasket, and a 0.010-inch thick furan cathode gasket. The gasket is placed around the flow fields next to the electrode/diffusion layers to create a seal to prevent gas leakage.

Fig. 97: Gaskets, end plate, and MEA for PEMFC

  - End plates

Fig. 98: End and flow field plates, gaskets, current collectors, and MEA for a single-cell PEMFC stack

- Conclusion of Fuel Cell components

Fig. 99: Resumed the materials needed for our fuel cell

- Bipolar plate design

The description of the design :

Active area dimensions: 22 x 26 cm

Total Area Dimensions: 23.1 x 29 cm

Overall Dimensions (L x W x D): 30 x 30 x 0.4 cm

Graphite Plate Side A & B:

• Depth of Flow Fields: 0.75 mm
  • Length Per Flow Field: 223.6 cm
  • Number of Flow Field Lines: 6
  • Total Length of Flow Fields: ~13.4 m

Fig. 100: Sizing of our fuel cell design

- Components costs of one cell

  - PEMFC

Active Area Dimensions: 5 x 5 cm (1.97" x 1.97")

Active Area: 25 cm2 (or 3.87 in2)

Flow Pattern or Channel Design: Serpentine (5-channels)

Total Physical Dimensions for Graphite Plates: 9.6 x 9.6 cm (3.77" x 3.77")

Thickness of the Graphite Plates: 1.9 cm (0.75")

  - MEA

Item #1:

These Reversible Membrane Electrode Assemblies (MEA) can be used as in an Electrolyzer for Hydrogen production or in Polymer Electrolyte Fuel Cell (PEMFC) for electricity production.  Perfect for educational products or demonstrations of the advantages of hydrogen as an energy storage medium.  We can assist with additional customization as well as the unique design aspects of Reversible Fuel Cell / Electrolyzer systems.  These Reversible MEAs come in a 3-Layer configuration, also known as a Catalyst Coated Membrane (CCM).

Item #2:

3-Layer, Catalyst Coated Membrane Electrode Assembly (MEA) for use in Hydrogen/Air Fuel Cells.  One of the most economical and cost effective MEAs on the market, the standard configuration features a mid-range Platinum loading (0.5 mg/cm²) on a 0.002” membrane (Nafion® 212). Custom sizes and configurations are also available with no minimum order quantities and typical lead times of 1 to 5 business days, even for custom configurations. These Hydrogen Air MEAs are 3-Layer.

Item #3:

This 5-Layer Membrane Electrode Assembly (MEA) is the standard MEA for use in the PEM Research Test Cell - 250cm². Please contact us for custom configurations.

Specifications:

• Custom Die Cut to fit
• Membrane Type: Nafion™ 212
• Active Area: 256.5 x 97.5 mm
• Membrane Area: 310 x 115 mm
• Anode Loading & Catalyst: 0.3 mg/cm² Platinum on Carbon 40%
• Cathode Loading & Catalyst: 0.3 mg/cm² Platinum on Carbon 40%
• Gas Diffusion Layer: Sigracet 28BC
• Gas Diffusion Layer Type : Carbon Paper

Item #4:

High performance Polymer Electrolyte Fuel Cell (PEMFC) Membrane Electrode Assembly (MEA) where performance and efficiency is critical. They can be used in Hydrogen/Air or Hydrogen/Oxygen fuel cells.  The most economical high performance MEA on the market, the standard configuration features a high Platinum loading (4 mg/cm²) and a 0.005” membrane (Nafion™ 115) with a 365 um thick carbon cloth GDL (others available). Custom sizes and configurations are also available with no minimum order quantities and typical lead times of 1 to 5 days, even for custom configurations. These Hydrogen Oxygen MEAs are 5-Layer.

### 21.2.1. Nafion for Electrolyte

Item #1:

Nafion™ HP membranes are ultra-thin cation exchange membranes that are manufactured by the Chemours Company.  These membranes are reinforced and designed for lower relative humidity environments and high operating temperature. The reinforcement improves the membrane’s handling and physical properties. When the reinforcement is combined with the chemically stabilized polymer, the Nafion™ HP membrane exhibits both substantially lower fluoride ion release and longer operating durability under challenging fuel cell conditions. Nafion™ HP is 20.3 micrometers (0.8 mil) thick. The membrane is positioned between a backing film and a coversheet.

Item #2:

Nafion™ Membrane is used to separate the anode and cathode compartment of Proton Exchange Membrane fuel cells and water electrolyzers. The thickness of this particular cation exchange membrane, Nafion™ 117 makes it suitable for Direct Methanol Fuel Cells (DMFC). Nafion™ 117 is 183 micrometers (7.2 mil) thick.

Chemours (formerly DuPont) Nafion™ 117 membranes are non-reinforced films based on chemically stabilized perfluorosulfonic acid/PTFE copolymer in the acid (H+) form. The physical properties remain the same for the chemically stabilized membranes, which exhibit substantially lower fluoride ion release compared to the non-stabilized polymer – a sign of improved chemical durability. Nafion™ PFSA membranes are widely used for Proton Exchange Membrane (PEM) fuel cells and water electrolyzers. The membrane performs as a separator and solid electrolyte in a variety of electrochemical cells that require the membrane to selectively transport cations across the cell junction. The polymer is chemically resistant and durable.

Item #3:

Nafion™ Membrane is used to separate the anode and cathode compartment of Proton Exchange Membrane fuel cells and water electrolyzers. The thickness of this particular cation exchange membrane, Nafion™ 212 makes it suitable for many Hydrogen Air/Oxygen Fuel Cell applications. Nafion™ 212 is 50.8 micrometers (2 mil) thick. The membrane is positioned between a backing film and a coversheet.

Chemours (formerly DuPont) Nafion™ PFSA NR-212 membranes are based on chemically stabilized perfluorosulfonic acid/PTFE copolymer in the acid (H+) form, and exhibit substantially lower fluoride ion release compared to the non-stabilized polymer – a sign of improved chemical durability. Nafion™ PFSA membranes are widely used for Proton Exchange Membrane (PEM) fuel cells and water electrolyzers. The membrane performs as a separator and solid electrolyte in a variety of electrochemical cells that require the membrane to selectively transport cations across the cell junction. The polymer is chemically resistant and durable.

### 21.2.2. Carbon paper for GDL

Freudenberg H14 is a flexible and easy to use base carbon paper Gas Diffusion Layer (GDL) without a Microporous Layer (MPL) and without a hydrophobic treatment.  It is 150 um (microns) thick.

Freudenberg H14 is formerly known as H1410.

### 21.2.3. GDL+Catalyst

A low-cost electrode utilizing a woven carbon cloth substrate and a 20% Platinum on Vulcan Carbon support catalyst.  This low loading is designed for cost sensitive applications and is suitable for electrochemical systems needing low amounts of Platinum to support the reaction.  This electrode is perfect for Hydrogen/Air Fuel Cell applications where the extra cost of the higher loading GDE may not be justified. The Gas Diffusion Layer (GDL) used is a standard carbon cloth with MPL which is 365 microns thick. Other GDL materials are also available by custom request, as are custom sizes and loadings.

Includes a Nafion Post Coat for improved water management and adhesion to the membrane.

0.2 mg/cm² 20% Platinum on Vulcan - Carbon Cloth Electrode (W1S1009) has been discontinued and was permanently replaced by 0.2 mg/cm² 20% Platinum on Vulcan - Carbon Cloth Electrode (W1S1010).

  - Bipolar plate

Item #1:

Fuel Cell Grade Graphite Plates can be machined on both sides to be used as bi-polar plates. These plates exhibit high electrical and thermal conductivity, incredible resistance to chemicals, and are densified and resin-filled for low permeability.

Length x Width: 12.0"x 12.0"

Thickness Tolerance: +0.125" / -0"

Length and Width Tolerance: +0.75" / -0"

Item #2:

These Isomolded Graphite Plates can be machined on both sides.  Isomolded plates are made out of very fine grain, high strength and density graphite.  These plates are Isostatically pressed.

Size - 12.0" x 12.0"

Thickness Tolerance +/- 0.001"

Length and Width Tolerance +/- 0.005"

Item #3:

These Isomolded Graphite Plates can be machined on both sides.  Isomolded plates are made out of very fine grain, high strength and density graphite.  These plates are Isostatically pressed.

Size - 8.0" x 8.0"

Thickness Tolerance +/- 0.001"

Length and Width Tolerance +/- 0.005"

Item #4:

These Isomolded Graphite Plates can be machined on both sides.  Isomolded plates are made out of very fine grain, high strength and density graphite.  These plates are Isostatically pressed.

Size - 6.0" x 6.0"

Thickness Tolerance +/- 0.001"

Length and Width Tolerance +/- 0.005"

Item #5:

Fuel Cell Grade Graphite Plates can be machined on both sides to be used as bi-polar plates.  The materials used in production allow for very high fuel cell performance.  Continuous compound production permits homogeneity and high material quality.  These bipolar plates allow fuel cells to operate at high temperatures and have excellent electrical and thermal conductivity.

Length x Width - 4"x 4"

Thickness - 5mm (0.197")

These closed bipolar graphite plates can be used as replacements plates for the Flex-Stak Electrochemical Cell, or you can use them as the basis to build your own closed fuel cell.

Active Area Dimensions: 3.2 x 3.2 cm

Total Area Dimensions: 5.3 x 5.3 cm

Overall Dimensions (L x W x D): 6.3 x 6.3 x 0.4 cm

Graphite Plate Specifications:

• Depth of Flow Fields: 0.75 mm
• Length Per Flow Field: 30 mm
• Number of Flow Field Lines: 8
• Total Length of Flow Fields: 240 mm

Item #6:

10 cm2 Open Bipolar Graphite plate suitable for small Hydrogen / Air Fuel Cells and Methanol Fuel Cells.  These bipolar plates can be used as replacement components for the Parker TekStak or the Flex-Stak series fuel cells, or you can use them as the basis to build your own open fuel cell.

They incorporate a parallel path design for even hydrogen or methanol distribution and a straight channel design on the reverse side for Air supply and cooling of the fuel cell.  These cells can be used in conjuction with the older

Perfect for replacement parts or to experiment with your own designs.

Active Area Dimensions: 3.2 x 3.2 cm

Total Area Dimensions: 5.3 x 5.3 cm

Overall Dimensions (L x W x D): 6.3 x 6.3 x 0.4 cm

| Graphite Plate Side A: • Depth of Flow Fields: 2 mm • Length Per Flow Field: 54 mm • Number of Flow Field Lines: 8 • Total Length of Flow Fields: 432 mm | Graphite Plate Side B: • Depth of Flow Fields: 0.75 mm • Length Per Flow Field: 30 mm • Number of Flow Field Lines: 8 • Total Length of Flow Fields: 240 mm |
| --- | --- |

  - Gaskets

Item #1:

Thin gauge 12 x 12 inch Silicone Rubber Gasketing for use in fuel cell fixtures.  Like other silicone, this rubber stays flexible over a wide temperature range, but its softness gives it better conformability than other rubber.  A peel-off protective masking keeps this rubber free from dust and debris. Width and length tolerances are ±1/4".  Durometer tolerance is ±5.

Teflon and fiberglass reinforced Teflon are used in high temperature applications such as High Temperature Polymer Electrolyte Membrane Fuel Cells (HT-PEMFC) and Phosphoric Acid Fuel Cells (PAFC).

HT6135 Silicon gasketing is a solid silicone elastomer.  Silicone elastomers exhibit a natural shrinkage when the carrier or liner is removed.  Thickness measurements do not include carrier or liner.

Item #2:

Cut your own gaskets out of this 12 inch x 12 inch sheet of high-performance EPDM (Ethylene Propylene Diene Monomer) Rubber.  Provides excellent seals for both Hydrogen and Direct Methanol fuel cells.

With greater strength than standard Weather-Resistant EPDM Rubber, these sheets provide better shock-absorbing qualities and longer life. They are resistant to sunlight, ozone, and water.

EPDM Rubber is peroxide cured for increased temperature resistance.

  - Current plate

  - End plate

This Garolite sheet can be used to make fuel cell end plates. This Garolite grade is the flame-retardant version of G-10 Garolite, offering excellent strength, low water absorption, and good electrical insulating qualities in dry and humid conditions.  The material is fiberglass-cloth with a flame-retardant epoxy resin.  It meets MIL-I-24768/27 and UL 94V0 for flame retardance.

These sheets are unmachined and generally come in a black, blue, or tan color.

Thickness Tolerance

At 1/16" ±0.008"

At 1/8"   ±0.012"

At 1/4"   ±0.022"

At 3/8"   ±0.038"

Width and Length Tolerances ±1/4"

This Garolite sheet can be used to make fuel cell end plates. This Garolite grade is the flame-retardant version of G-10 Garolite, offering excellent strength, low water absorption, and good electrical insulating qualities in dry and humid conditions.  The material is fiberglass-cloth with a flame-retardant epoxy resin.  It meets MIL-I-24768/27 and UL 94V0 for flame retardance.

These sheets are unmachined and generally come in a black, blue, or tan color.

Thickness Tolerance

At 1/16" ±0.008"

At 1/8"   ±0.012"

At 1/4"   ±0.022"

At 3/8"   ±0.038"

Width and Length Tolerances ±1/4"

# Description of our prototype fuel cell system

  - Existing electrical system

The electrical system in the prototype consists of the low voltage (12 V) DC system.

  - Fuel cell stack

The parameter that will be crucial for the size of the stack is the maximum power that should be delivered. As an example, a maximum power level of 1 kW is chosen.

    - Size

The first step to obtain the size of the fuel cell stack is to calculate the number of cells needed to deliver a specific voltage level. The cell voltage is chosen to 0.7 V based on the voltage-current density graph seen in Figure 101. At 0.7 V the power is about its maximum value. In this example the needed voltage will be assumed to be 12 V. The number of cells will be 18 (17.143) when the fuel cells produce this voltage.

Fig. 101: Voltage-current density diagram for a low temperature, air pressure fuel cell

The total current from the stack when supplying the maximum power can now be calculated.

P= U x I	→	I = PU = 100012*18 = 4.63 A		(42)

Where, P = Power [W]

U = Voltage [V]

I = Current [A]

For a specific power rate, the current can be increased or decreased, depending on the need of the load, if the voltage is altered by changing the number of cells. If the needed voltage is different from the stack voltage, a voltage regulator could be used to achieve the right level.

From Figure 101 it can be found that the current density for 0.7 V is around 550 mA/cm2. The area of each cell can now be calculated using the current calculated in equation (42).

A = IJ = 4.630.55 = 8.42 cm2			(43)

Where,

A = Fuel cell area [cm2]

J = Current density [A/cm2]

The total size of the stack depends on this area, the number of cells and the thickness of each cell. This thickness depends on material and design.

    - Fuel cell types

There are two main groups of cells that are available, low temperature and high temperature fuel cells. What determines which type to use is the field of application. In low temperature cells the hydrogen has to be more pure than in the other case. In the case of high temperature cells, hydrogen can be produced internally in the stack by reforming other fuels, such as Liquefied Petroleum Gas (LPG), methanol, etc.

In this prototype, we are looking to fuel cell generates electrical power from hydrogen gas and humid air. There is no need for high temperature so the suitable type for our prototype is PEMFC low temperature.

  - Converters

    - DC/DC converter

In the calculations on the fuel cell stack the number of cells is chosen with respect to that the voltage over the stack should have the same voltage as the grid voltage. If for some reason the number of cells is chosen differently a DC/DC converter can be used to achieve the right output voltage level.

The voltage over the stack is normally not constant and when the current increases there will be a voltage drop. In fuel cells this voltage drop is greater than in normal electrical power generators. In this case there is also need for a DC/DC converter to solve this problem.

    - DC/AC inverter

As mentioned before on fuel cells the output from a stack is a DC current. When using a DC/AC inverter there is no use for a DC/DC converter because it is also capable of regulating the output voltage level.

  - Hydrogen storage

To be able to use hydrogen as a fuel, there are different ways of achieving this and the most common ways are by buying H2 tubes, by using an electrolyzer or by using a reformer. In this project, hydrogen gas was obtained from the electrolyzer.

An interesting observation to keep in mind is that hydrogen will take a lot of room at low pressures. To illustrate how the density varies with the pressure, an example is that 1 m3 contains 0.1 kg H2 at a pressure of 1 bar and 15 kg H2 at a pressure of 200 bar. Another interesting fact is that one kilogram of hydrogen has the same energy content as one gallon (about 4 liters) of gasoline.

- Using an Electrolyzer

The theory of this is based on the electrolysis of water. By letting a current pass through the water, hydrogen and oxygen are separated. With this method the hydrogen is produced with an electrolyzer and is stored in tubes. The greatest advantage of this method is that the produced hydrogen is very pure.

  - Energy and fuel estimation

The objective of this paragraph is to calculate the quantity of fuel needed for the fuel cells to deliver power during an estimated time. The first step is to find out the energy consumed for the level below 1 kW, i.e. the power which the fuel cells will provide. The energy was supposed to be about 10 kWh/day (24 hours).

The energy content LHV (Low Heating Value) in one kilogram of hydrogen at room temperature and at atmospheric pressure is around 120 MJ which equals 33.3 kWh ( H2 E ).

Eone day = 10 x 1 = 10 kWh 		  (44)

m = E (one day)E (H2) = 1033.3 = 0.3 Kg    		(45)

Where,

Eone day = Energy during one day delivered by the fuel cell system [kWh]

EH2 = Energy content of one Kg of H2 [kWh]

m = Mass of the hydrogen [Kg]

As said before electrolyzer delivers hydrogen gas at a pressure of 1 bar. At this pressure the volume needed for 0.1 kg of H2 is 1 m3. the mass needed for one day has a volume of thirteen of a cubic meter (13000 dm3) with this pressure. This volume can be decreased if a higher pressure is used.

if hydrogen gas is available at a pressure of 200 bar. At this pressure the volume needed for 15 kg of H2 is 1 m3. It is easy to see that the mass needed for one day has a volume of 0.087 m3 (87 dm3) with this pressure.

  - FreeCAD design

    - Bipolar plate design

- Design details

    - Gasket design

- Design details

    - MEA design

- Design details

  - Specification of requirements

-------------------------------------------------------------------

Literature

…

# References

[1] Mikkola, Mikko. “Experimental Studies on Polymer Electrolyte Membrane Fuel Cell Stacks.” Helinski University of Technology, Department of Engineering Physics and Mathematics, Masters Thesis, 2001.

[2] Lin, Bruce. “Conceptual Design and Modeling of a Fuel Cell Scooter for Urban Asia.” Princeton University, Masters Thesis, 1999.

[3] Hussain, M.M., J.J. Baschuk, X. Li, and I. Dincer. “Thermodynamic Analysis of a PEM Fuel Cell Power System.” International Journal of Thermal Sciences. 2005. Vol. 44, pp. 903–911.

[4] O’Hayre, Ryan, Suk-Won Cha, Whitney Colella, and Fritz B. Prinz. Fuel Cell Fundamentals. 2006. New York: John Wiley & Sons.

[5] Ibid.

[6] J.G. Carton and A.G. Olab, “Design of experiment study of the parameters that affect performance of three flow plate configurations of a proton exchange membrane fuel cell”, Energy, 35 (7), pp 2796-2806, 2010.

[7] B. C. Steele and A. Heinzel, “Materials for fuel-cell technologies,” Nature, vol. 414, no. 6861, pp. 345–352, 2001.

[8] J. Zhang, J. Wu, H. Zhang, and J. Zhang, Pem Fuel Cell Testing and Diagnosis, Elsevier, Oxford, UK, 2013.

[9] R. O'Hayre, S-.W. Cha, W. Colella, and B. F. Prinz, Fuel Cell Fundamentals, John Wiley & Sons, Oxford, UK, 2nd edition, 2009.

[10] M. Ji and Z. Wei, “A review of water management in polymer electrolyte membrane fuel cells,” Energies, vol. 2, no. 4, pp. 1057–1106, 2009.

https://www.researchgate.net/publication/309898224_A_review_on_prognostics_and_health_monitoring_of_proton_exchange_membrane_fuel_cell/download

https://www1.eere.energy.gov/hydrogenandfuelcells/pdfs/fct_h2_fuelcell_factsheet.pdf

https://www.youtube.com/watch?v=yrAAVOgBmcE

https://www.energy.gov/eere/fuelcells/fuel-cells

https://www.sciencedirect.com/book/9780123742599/pem-fuel-cell-modeling-and-simulation-using-matlab

https://www.fuelcellstore.com/fuel-cell-education-products/educational-media/designing-and-building-fuel-cells-Speigel-hardcover

https://www.scribd.com/document/447288677/Design-and-Control-of-Fuel-Cell-System-for-Tran-z-lib-org-pdf

https://bz.vdma.org/documents/266669/49673320/FuelCellProductionBrochures_FuelCellComponents_Edition1_online_en_PEM_v07_scn_1606398023504.pdf/35fca3ae-b8e5-37e6-a685-d2dcae8a3d15

https://www1.eere.energy.gov/hydrogenandfuelcells/pdfs/fct_h2_fuelcell_factsheet.pdf

https://bz.vdma.org/documents/266669/49673320/FuelCellProductionBrochures_FuelCellComponents_Edition1_online_en_PEM_v07_scn_1606398023504.pdf/35fca3ae-b8e5-37e6-a685-d2dcae8a3d15

file:///C:/Users/admin/AppData/Local/Temp/ThermalEngineeringPerfEvaluationofaPEMFCstackatpartialload.pdf

https://www.researchgate.net/publication/341095046_IMPACT_OF_PRESSURE_ON_THE_PERFORMANCE_OF_PROTON_EXCHANGE_MEMBRANE_FUEL_CELL

https://www.researchgate.net/publication/265412592_Design_and_Development_of_Proton_Exchange_Membrane_Fuel_Cell_using_Open_Pore_Cellular_Foam_as_Flow_Plate_Material/download

https://wlv.openrepository.com/bitstream/handle/2436/621478/AAM-A%20Baroutaji-%20Developments%20of%20electric%20cars%20and%20fuel%20cell%20hydrogen%20electric%20cars-Wire.pdf?sequence=8

https://www.researchgate.net/publication/282896560_Proton_Exchange_Membrane_Fuel_Cell_Technology_India's_Perspective/download

https://www.hindawi.com/journals/jen/2019/3821082/

https://www.fuelcellstore.com/blog-section/fuel-cell-materials-blog-articles/membrane-comparison-chart-2021

https://www.mdpi.com/1996-1073/11/11/3203/htm

https://www.fuelcellstore.com/fuel-cell-components/membrane-electrode-assembly/reversible-fuel-cell-ccm

https://www.fuelcellstore.com/fuel-cell-components/membrane-electrode-assembly/ha-ccm

https://www.fuelcellstore.com/fuel-cell-components/membrane-electrode-assembly/mea-pem-research-test-cell-250cm

https://www.fuelcellstore.com/fuel-cell-components/membrane-electrode-assembly/hydrogen-oxygen-mea

https://www.fuelcellstore.com/fuel-cell-components/nafion-hp?sort=p.sort_order&order=ASC

https://www.fuelcellstore.com/nafion-117

https://www.fuelcellstore.com/nafion-212

https://www.fuelcellstore.com/fuel-cell-components/freudenberg-h1410?sort=p.model&order=ASC

https://www.fuelcellstore.com/fuel-cell-components/carbon-cloth-02-ptc-gas-diffusion-electrode-w1s1010?sort=p.sort_order&order=ASC

https://www.fuelcellstore.com/impervious-bipolar-graphite-plates

https://www.fuelcellstore.com/isomolded-plate-144

https://www.fuelcellstore.com/isomolded-plate-064

https://www.fuelcellstore.com/isomolded-plate-036

https://www.fuelcellstore.com/bipolar-plate-5mm

https://www.fuelcellstore.com/flex-stak-anode-bipolar-plate?search=Bipolar%20Graphite%20Plate

https://www.fuelcellstore.com/fuel-cell-components/plates/flex-stack-bipolar-graphite-plate

https://www.fuelcellstore.com/fuel-cell-components/gaskets/silicone-gasket-35a?sort=p.model&order=ASC

https://www.fuelcellstore.com/epdm-rubber-50A

https://www.fuelcellstore.com/fuel-cell-components/plates/end-plates/garolite-sheet-144

https://www.fuelcellstore.com/fuel-cell-components/plates/end-plates/garolite-sheet-036

https://www.slideserve.com/Mercy/pem-fuel-cell-stack-sealing-powerpoint-ppt-presentation

https://www.google.com/imgres?imgurl=http%3A%2F%2Fwww.hhomart.com%2Fimg%2Fcms%2FPEMFC%2520500w%2520Specs.jpg&imgrefurl=https%3A%2F%2Fwww.hhomart.com%2Fen%2Ffuellcell%2F6-500w-pem-fuel-cell-stack.html&tbnid=0ZzJW5PkHVmXeM&vet=12ahUKEwi9ga6k7JnzAhUPTBoKHSmHBHwQMygZegUIARDSAQ..i&docid=EmtxcOEaOV26XM&w=2066&h=2725&q=dimension%20of%20fuel%20cell&client=firefox-b-d&ved=2ahUKEwi9ga6k7JnzAhUPTBoKHSmHBHwQMygZegUIARDSAQ

https://fuelcellsworks.com/news/throwback-thursday-spotlight-horizon-automotive-pem-fuel-cells-to-set-300kw-benchmark/